## Slide 1: Characterization of Ga2O3 Single Crystal and Thin Films
Emily Hommerding
August 13, 2012
NSF REU
Bermudez, V.m. "The Structure of Low-index Surfaces of β-Ga2O3." Chemical Physics323.2-3 (2006): 193-203.

## Slide 2
Anisotropic
Unique in that it is transparent, yet conducting
Conductivity and transparency are related to the dielectric constant
Dielectric constant not yet determined
Ga2O3
Bermudez, V.m. "The Structure of Low-index Surfaces of β-Ga2O3." Chemical Physics323.2-3 (2006): 193-203.

## Slide 3: XPS : X-Ray Photoelectron Spectroscopy
Sample in UHV
X-rays
Cylindrical Hemispherical Analyzer
Ar Sputter Gun
A sample is put in UHV
Incoming x-rays hit the sample
Electrons leave the sample
Electron’s KE is measured by the CHA
Argon ions can sputter the sample

## Slide 4
Generation of a Photoelectron
1s
2s
2p
EFermi
Conduction Band
Valence Band
Vacuum
hν

## Slide 5
Conservation of Energy Equation for XPS
Energy of the incoming x-ray
(k-α of Al)
Kinetic energy of the electron that has been excited from the sample
Work function of the spectrometer used to measure kinetic energy
Binding energy of the electron in an atom on the surface
Fadley, Charles S. "X-ray Photoelectron Spectroscopy: From Origins to Future Directions." Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment 601.1-2 (2009): 8-31.

## Slide 6: XPS / Sputtering Application
Pd deposited on the surface
The Goal: Gradually sputter away a spot of Pd for a future application
Sputter Gun

## Slide 7
0
100
200
300
400
500
600
700
800
900
1000
0
0.5
1
1.5
2
2.5
x 10
5
Binding Energy (eV)
c/s
XPS Line Scan of the Sputtered Spot
330
332
334
336
338
340
342
344
346
348
350
0
0.5
1
1.5
2
2.5
3
3.5
4
x 10
4
Binding Energy (eV)
c/s
1110
1112
1114
1116
1118
1120
1122
1124
1126
1128
1130
0
2
4
6
8
10
12
14
16
x 10
4
Binding Energy (eV)
c/s
1
2
3
4
5
6
Pd surface coating
Sputtered Spot
Survey Scan
Ga 2p high resolution scan
Pd High resolution Scan
1
6
1
6
1
6

## Slide 8
UV Visible Spectroscopy
UV light passes through a sample
A detector lies behind the sample
The percent of light transmitted through the system at a given wavelength is measured and compared with a reference beam
Oliva, Brittany L., and Andrew R. Barron. "Connexions." Connexions. Rice University, 5 June 2010. Web. 27 July 2012. <http://cnx.org/content/m34525/latest/>.

## Slide 9: Optical Constants, Band Gap
Where d is the thickness and
Optical Absorption Coefficient
The band gap is related to the optical absorption coefficient in the following way

## Slide 10
Rotations of the single crystal produce differing optical properties!
00

## Slide 11: Ellipsometry
Light Source
Polarizer
Linearly Polarized Light Incident on Sample
Elliptically Polarized Light Leaves Sample
Detector
Sample
Incident linearly polarized light of known polarization and amplitude is reflected off the top surface of a sample. Reflected light is elliptically polarized and has a change in amplitude
Analyzer
Variable angle of incidence
"Light & Materials - Part I." Spectroscopic Ellipsometry Tutorial Light and Materials I. J.A. WOOLLAM CO. INC, n.d. Web. 31 July 2012. <http://www.jawoollam.com/tutorial_2.html>.

## Slide 12
Optical Properties
Dielectric Constant
Index of Refraction
Optical Absorption Coefficient (again)
The phase velocity of light slows down in a material
The optical absorption coefficient is the same as was used to extract band gap information in UV-Visible Spectroscopy
The index of refraction and dielectric constant are related
Ellipsometry can be used to determine..
Optical constants
Thickness
Composition
Crystallinity

## Slide 13
Amplitude
Phase
Fresnel Reflectivity Equations
An electric field parallel to the plane of incidence is p-polarized, and perpendicular is s-polarized
Reflected parallel
Reflected perpendicular
Notes: Remember how UV-Vis showed us that optical properties in Ga2O3 differed based on crystal orientation?
Ellipsometry can be used to extract information about optical constants in Ga2O3 in varying directions w.r.t the optical axis.
Analysis of single crystal Ga2O3 can set a standard for analysis of thin films of Ga2O3.
We will be able to differentiate between amorphous and crystalline thin film samples. "Type equation here."

## Slide 14
Single Crystal Ga2O3 Ellipsometry Data at One Orientation
Something is ‘turning on’ just under 5eV .. close to Ga2O3’s band gap!
Angles refer to angle of incidence
Next steps…
Plot data from other orientations of the single crystal
Use a model to achieve a fit that works for each orientation

## Slide 15
A relatively good fit for three crystal orientations and three angles of incidence is achieved, and the resulting dielectric constants are plotted
Two oscillator models are used to fit the data
Ga2O3 Single Crystal Ellipsometry at Three Orientations

## Slide 16: Compare Single Crystal Results to Thin Films
Can we differentiate a crystalline Ga2O3 thin film sample from an amorphous one?
Films were deposited on a Si substrate, so it is useful to first examine the substrate by itself
Dielectric constants of Si from literature
Adachi, Sadao. "Model Dielectric Constants of Si and Ge." Physical Review B 38.18 (1988): 12966-2976.

## Slide 17
Ga2O3 Thin Film Results
Ga2O3 Nominally 100nm thin film deposited on Si; Expected to be amorphous
Ga2O3 Nominally 100nm thin film deposited on Si & annealed; Expected to be polycrystalline

## Slide 18
Dielectric Constants
Modeled using B-Spline with Kramers-Kronig analysis
Thickness = 128 nm Roughness = 9 nm
Nominally amorphous film
Nominally polycrystalline film
Modeled using a Psemi M0 oscillator and a Cody Lorentz oscillator
Thickness = 156 nm Roughness =13 nm

## Slide 19
Conclusion
Ellipsometry is a quick optical technique which can determine many material properties and optical constants
Ga2O3’s unique properties can be explored for future device applications
XPS is a powerful tool for examining surface and interface features
UV-Vis can measure band gaps and identify anisotropy

## Slide 20: Acknowledgements
A special thanks to Marjorie Olmstead and Fumio Ohuchi for advising me in this project
Thanks to Alejandro Garcia and Subhadeep Gupta and the NSF for facilitating the REU program

## Slide 21: May I have your questions?