## Slide 1: Effects of Strain on Vanadium Dioxide Nanobeams
Eli Bingham
University of North Carolina
UW REU 2012
Advisor: David Cobden

## Slide 2: Overview of VO2
Strongly correlated
  Band theory breaks down when electrons interact
Metal-insulator transition
  Dramatic (4 orders of magnitude)
  Ultrafast (~100fs)
  Near room T (bulk Tc = 68C)
Applications
  Ultrafast optical shutters
  Mott transistor
  Model system for other strongly correlated materials

## Slide 4: Structure (V atoms only)
a
1.016 a
1.011 a
R (metallic)
M2 (insulator)
M1 (insulator)
c-axis
Notes: VO2 has been noted for the proximity of its transition temperature to the room temperature, at which the conductivity changes by more than four orders of magnitude. The transition also involves structural change from high temperature rutile to low temperature monoclinic. After some time, it was found that there was more than one insulating phase, namely M2. The key thing to note here is the different lattice constant along the rutile c-axis of the different phases. M1 is about a percent longer than the rutile and M2 about 1.6 percent.

## Slide 5: Why nanowires?
Single domains
Simple nucleation
Precise control of strain
Durable

## Slide 6: Phase diagram
Not well understood
  Main tools: X-ray diffraction, Raman spectroscopy
Triple point location unknown – difficult to pinpoint in bulk
  Very close to bulk Tc and zero strain, but not equal
Mysterious hysteresis in cooling
Role of doping?
Triclinic: phase or mixture?

## Slide 7
M
R
R
M
Fixed length L
High elastic cost
R
M
R
M
ΔL
Δx
Changing L
Notes: Unlike a VO2 beam that is free, a VO2 beam suspended this way does not turn metallic instantly. Instead it shows coexistence. Remember that the rutile phase is shorter than the monoclinic. If the whole domain changed to the rutile while preserving the length, it would be under very high tensile strain. Instead the system settles by going into coexistence at the cost of interphase boundary creation.
Now sitting at the coexistence, what happens if you change the length of the whole system? At the phase boundary, change in the strain along the beam is compensated by introconversion of the two phases with different lattice constants.

## Slide 8: Fabrication
SiO2-Si wafers
Gold contacts placed via photolithography
20 or 40 micron gap etched away
Wire placed across gap with nanomanipulator
Indium contacts from wire to gold
Fix with epoxy
  UVC? UVC + heat cure? TEOS? FIB?

## Slide 11: Experimental setup

## Slide 12: Measurements
Interphase boundary position vs laser position
Isobaric
Isothermal
Holding constant boundary position
Electrical transport (R-T)
Notes: One of the first groups to see M1-M2 boundary optically

## Slide 13
Constant x

## Slide 17: Results (preliminary)
Data support triple point below bulk Tc
Ratios of boundary position-laser position slopes allow calculation of relative lattice constants
Direct measurement of undoped phase diagram promising but inconclusive
  More/better data needed

## Slide 18: Aluminum Doping
How to stabilize M2 phase at room temperature?
Effects of doping on phase diagram?
Poorly documented in literature
  Focus on lowering Tc for smart windows (W)
  Al doping mainly studied in bulk crystals
Region of interest entirely compressive

## Slide 19
Al-doped VO2

## Slide 20: Future work
Improved devices
  New transfer technique, no indium or epoxy
Improved strain setup
  New laser/piezo, integrate Raman into setup
Strain-free devices
Strain other materials
  Graphene, MoSe2, MoS2, BN
Tunneling spectroscopy of VO2
Ultrafast pump-probe measurement of MIT on various substrates